## Slide 1
The Use of Scanning Electron Microscopy (SEM)
for Microstructural Characterization
and Failure Analysis of Materials
Saif Elsaady
MSE 550 — Advanced Materials Characterization | Dr. Theodore | April 4, 2026
1

## Slide 2
Introduction to Scanning Electron Microscopy
SEM uses a focused electron beam to probe specimen surfaces, generating multiple signals that carry information about structure, composition, and electronic properties
Secondary electrons (SEs) provide surface topographic contrast at high resolution
Backscattered electrons (BSEs) reveal compositional differences due to atomic number variations
Characteristic X-rays enable elemental identification via Energy Dispersive Spectroscopy (EDS)
Cathodoluminescence (CL) provides information about band-gap structure, defects, and impurity distributions
The integration of multiple signal detection modes gives SEM a unique and irreplaceable role in materials characterization
Jiang, R. et al. (2024). Frontiers of Materials Science, 18(4), Article 240709.
2

## Slide 3
Evolution of SEM: From Imaging to Quantitative Analysis
SEM has evolved from a qualitative imaging tool into a robust quantitative analytical instrument
Advances driven by improvements in electron source technology, detector design, and digital image analysis
Correlative microscopy combines SEM-EDS with X-ray computed tomography (XCT) and nanoindentation for comprehensive characterization
SEM-based fractography has become increasingly sophisticated for failure analysis
Computational methods now enable quantitative evaluation of fatigue striations for predictive capability
Huang et al. (2023). Materials Characterization, 205, 113331; Maruschak & Maruschak (2024). MethodsX, 13, 102989.
3

## Slide 4
Scope: Two Applications of SEM
Application 1
Microstructural Characterization
— Correlative microscopy of Aba Panu meteorite (SEM-EDS + XCT + nanoindentation)
— SEM-CL mapping of geological and semiconductor microstructures
Application 2
Failure Analysis & Fractography
— Qualitative SEM fractography of dental ceramics and polymers
— Computational methods for quantitative fatigue striation analysis
Huang et al. (2023); Jiang et al. (2024); Alghazzawi et al. (2023); Maruschak & Maruschak (2024).
4

## Slide 5
SEM Technique: Electron-Matter Interactions
Primary electron beam interacts with specimen atoms via elastic and inelastic scattering
Elastic scattering: electrons deflected by atomic nucleus with negligible energy loss → backscattered electrons (BSEs); probability increases with atomic number, providing compositional contrast
Inelastic scattering: energy transfer to specimen atoms → secondary electrons (SEs); low-energy electrons from shallow surface region, highly sensitive to topography
Inner-shell ionization produces characteristic X-rays as outer-shell electrons fill vacancies → elemental identification via EDS
Electron excitation of valence electrons generates cathodoluminescence (CL) photons sensitive to band-gap, defects, and impurities
Jiang, R. et al. (2024). Frontiers of Materials Science, 18(4), Article 240709; Huang et T.-J. et al. (2023). Materials Characterization, 205, 113331.
5

## Slide 6
SEM Detection Modes and Analytical Capabilities
Everhart-Thornley detector: standard SE imaging for surface topography
Solid-state diode detectors: BSE imaging for compositional (Z) contrast
Silicon drift detectors (SDDs): rapid EDS elemental analysis and mapping
EBSD: electron backscatter diffraction for crystallographic orientation analysis
FIB: focused ion beam milling for site-specific cross-sectioning and TEM sample preparation
High depth of field makes SEM ideal for examining rough or fractured surfaces
Huang et al. (2023). Materials Characterization, 205, 113331; Alghazzawi et al. (2023). Journal of Prosthodontics, 32(5), e100–e110.
6

## Slide 7
The SEM-CL System: Principle and Acquisition Modes
CL detector: aluminum-coated parabolic reflector beneath SEM pole piece collects luminescence photons from beam impact point
Panchromatic mode: captures total luminescence intensity across all wavelengths
Monochromatic mode: diffraction grating isolates specific wavelengths for selective phase imaging
Spectral imaging mode: wavelength-resolved spectra collected at each pixel during area scans
Angular resolution mode: maps directional emission of CL photons using back-projection from parabolic reflector geometry
Combined with BSE, EDS, and EBSD for comprehensive multimodal characterization from the same microregion
Jiang, R. et al. (2024). Frontiers of Materials Science, 18(4), Article 240709.
7

## Slide 8
SEM-CL Applications Across Material Systems
Geological mineralogy: mineral identification and classification using CL color variation, e.g., tracing origin of quartz grains based on defect structure
Halide perovskite research: monochromatic CL imaging distinguishes PbI₂ and perovskite phases that appear identical in SE images but exhibit distinct luminescence bands
Semiconductor analysis: mapping defect density, dislocation distributions, and local band-gap variations at nanoscale spatial resolution
Non-metallic inclusions: CL perspective may elucidate impact of oxides on microstructural phenomena such as composition segregation and grain orientation
Jiang, R. et al. (2024). Frontiers of Materials Science, 18(4), Article 240709.
8

## Slide 9
SEM for Fractographic Analysis
Fractography: examination of fracture surfaces to determine failure origins and propagation mechanisms
SEM's high depth of field and variable magnification make it the instrument of choice for identifying fracture features
Key features observed: failure origin, mirror region, mist, hackle lines, arrest lines, compression curl, and grain morphology
EDS at fracture origins can identify inclusions and contaminants responsible for failure initiation
Quantitative methods now enable automated measurement of fatigue striation parameters from SEM images
Alghazzawi et al. (2023). J. Prosthodontics, 32(5), e100–e110; Maruschak & Maruschak (2024). MethodsX, 13, 102989.
9

## Slide 10
Case Study 1: Correlative Microscopy of the Aba Panu Meteorite
Background & Motivation
Aba Panu: ordinary L3 chondrite meteorite that landed in Nigeria in 2018
Classified as minimal weathering (W0) and shock stage S4 — pristine condition ideal for microstructural investigation
Meteorite samples provide information about the formation history and environment of the early solar system
Multimodal, multiscale characterization is necessary to understand complex heterogeneous mineral assemblages
Approach: SEM-EDS combined with X-ray computed tomography (XCT) and nanoindentation
Huang, T.-J. et al. (2023). Materials Characterization, 205, Article 113331.
10

## Slide 11
Case Study 1: Experimental Setup
SEM-EDS:
Nova 200 NanoLab FEG SEM/FIB; specimens polished to 0.25 µm and Au-Pd coated
EDS mapping identified five mineral phases: olivine, pyroxene, chromite, kamacite, and troilite
XCT:
Zeiss Versa 520 X-ray microscope at 3.1 µm voxel size
3D reconstruction correlated with 2D SEM data to eliminate sampling bias
Nanoindentation:
Diamond Berkovich tip with continuous stiffness measurement (CSM)
Measured modulus and hardness of individual mineral phases
Huang, T.-J. et al. (2023). Materials Characterization, 205, Article 113331.
11

## Slide 12
Case Study 1: Key Results
Phase | Vol. % | Modulus (GPa) | Hardness (GPa)
Olivine | ~83.5% (combined) | 202.7 | 16.4
Pyroxene | with olivine | 175.9 | 12.7
Kamacite | ~1.9% | 211.3 | 3.3
Troilite | ~2.0% | 108.0 | 3.9
Key findings:
3D XCT revealed kamacite and troilite clusters preferentially distributed along chondrule rims
EDS line scans showed compositional gradient: decreasing Mg from olivine cores to dendritic matrix
Correlative approach provided comprehensive structural, compositional, and mechanical understanding
Huang, T.-J. et al. (2023). Materials Characterization, 205, Article 113331.
12

## Slide 13
Case Study 2: SEM Fractography for Failure Analysis
Background & Motivation
Fractography uses SEM to examine fracture surfaces and determine failure origins and mechanisms
Alghazzawi et al. studied dental ceramics (zirconia, glass-ceramics) and polymers (PEEK, PEKK, glass fiber composites) under standardized mechanical tests
Maruschak & Maruschak reviewed computational methods for quantifying fatigue striations on SEM images of polycrystalline materials
Goal: understand how SEM reveals manufacturing defects and predicts residual life under cyclic loading
Alghazzawi et al. (2023). J. Prosthodontics, 32(5); Maruschak & Maruschak (2024). MethodsX, 13, 102989.
13

## Slide 14
Case Study 2: Methods and Key Results
Qualitative Fractography
Tests: 4-pt bend, 3-pt bend, biaxial, crunch-the-crown
Zirconia bars: fracture origins at processing/sintering defects
Glass-ceramics: failure at surface flaws or fabrication voids
Polymers: PEKK showed ductile dimples then brittle propagation; fiber composites exposed glassy fibers
Critical flaws are a function of both material composition and loading geometry
Quantitative Striation Analysis
Multi-scale analysis: macro-, meso-, and micro-level fracture description
Striation step ∝ macroscopic crack length (linear in elastic-plastic FCG regime)
Machine learning methods now rank among the most promising for automated striation recognition
Fourier analysis, stereocouple methods, and 3D profile analysis address manual measurement limitations
Corrective D-factor needed when crack front growth is non-uniform
Alghazzawi et al. (2023). J. Prosthodontics, 32(5); Maruschak & Maruschak (2024). MethodsX, 13, 102989.
14

## Slide 15
Summary
SEM provides a versatile analytical platform capable of probing morphology, composition, crystallography, and optoelectronic properties from the same specimen region
Case Study 1: Correlative microscopy (SEM-EDS + XCT + nanoindentation) yielded comprehensive phase, compositional, and mechanical characterization of the Aba Panu meteorite; SEM-CL extends analytical reach to band-gap and defect mapping
Case Study 2: SEM fractography identified failure origins and manufacturing defects in dental materials; computational methods are transforming fractography from descriptive to predictive
As computational image analysis matures, SEM-based characterization will increasingly serve as both diagnostic and predictive across engineering, geological, biomedical, and semiconductor applications
15

## Slide 16
References
[1] Alghazzawi, T. F., Janowski, G. M., Ning, H., & Eberhardt, A. W. (2023). Qualitative SEM analysis of fracture surfaces for dental ceramics and polymers broken by flexural strength testing and crown compression. Journal of Prosthodontics, 32(5), e100–e110. https://doi.org/10.1111/jopr.13659
[2] Huang, T.-J., Niverty, S., Sundar, A., & Chawla, N. (2023). Microstructural characterization and mechanical behavior of Aba Panu meteorite by correlative microscopy and nanoindentation. Materials Characterization, 205, Article 113331. https://doi.org/10.1016/j.matchar.2023.113331
[3] Jiang, R., Yao, Y., Guan, J., Shen, J., Lu, H., & Li, M. (2024). Application of SEM-CL system in the characterization of material microstructures. Frontiers of Materials Science, 18(4), Article 240709. https://doi.org/10.1007/s11706-024-0709-5
[4] Maruschak, P., & Maruschak, O. (2024). Methods for evaluating fracture patterns of polycrystalline materials based on the parameter analysis of fatigue striations: A review. MethodsX, 13, Article 102989. https://doi.org/10.1016/j.mex.2024.102989
16

## Slide 17
Thank You
Thank you for your time and attention.
Saif Elsaady | MSE 550 | April 4, 2026
17